Magnetic interactions in Nd2PdSi3 and the formation of skyrmion phases in centrosymmetric metals

Viviane PEÇANHA-ANTONIO1,2, Zhaoyang SHAN3, Michael SMIDMAN3, Juba BOUAZIZ4, Bachir OULADDIAF5, Iurii KIBALIN5, Marie Helene LEMEE5, Christian BALZ2, Jakob LASS6, Daniel A. MAYOH7, Geetha BALAKRISHNAN7, Julie B. STAUNTON7, Devashibhai ADROJA2,8, Andrew T. BOOTHROYD1

1Department of Physics, University of Oxford, Clarendon Laboratory, Oxford OX1 3PU, United Kingdom

2ISIS Neutron and Muon Source, STFC Rutherford Appleton Laboratory, Didcot OX11 0QX, United Kingdom

3Center for Correlated Matter and School of Physics, Zhejiang University, Hangzhou 310058, China

4Department of Physics, The University of Tokyo, Bunkyo-ku, Tokyo, 113-0033, Japan

5Institut Laue-Langevin, 6 Rue Jules Horowitz, BP 156, 38042 Grenoble Cedx 9, France

6PSI Center for Neutron and Muon Sciences, 5232 Villigen PSI, Switzerland

7Department of Physics, University of Warwick, Coventry CV4 7AL, United Kingdom

8Highly Correlated Matter Research Group, Physics Department, University of Johannesburg, Auckland Park 2006, South Africa

We present an X-ray and neutron scattering study of the structure and magnetic excitations of Nd2PdSi3 [1], a sister compound of Gd2PdSi3 which was recently found to host a skyrmion phase despite its centrosymmetric crystal structure. Dispersive magnetic excitations corresponding to the complete crystal field scheme of the Nd atoms were measured throughout the reciprocal space Brillouin zone. The full measured spectrum was modelled by mean-field random-phase approximation (MF-RPA) to determine quantitatively the magnetic interactions between two distinct Nd sites. Our analysis finds that the exchange couplings in this system extend over large distances and are significantly affected by a crystallographic superstructure formed by ordering of the Pd and Si atoms. These results suggest that the skyrmion phase in Gd2PdSi3 is stabilised by long-range RKKY interactions rather than short-range triangular-lattice frustration. First principles theory results corroborate with a long-ranged RKKY interaction scenario, which has its basis in the complex, three-dimensional Fermi surface of this material.

[1] Peçanha-Antonio et al., arXiv:2504.10075v1

E-mail of the corresponding author: viviane.antonio@stfc.ac.uk