Kondo hybridization-driven topological phase transition in the Weyl semimetal candidate CeAlGe

Soohyeon Shin,1,2 Soonbeom Seo3, Igor Plokhikh,2 Jonathan S. White,2 Harim Jang4, Vladimir Y. Pomjakushin,2 Pascal Puphal,2 Yixi Su1, Tuson Park4, and Ekaterina Pomjakushina 2

1 Jülich Centre for Neutron Science (JCNS) at MLZ, Forschungszentrum Jülich GmbH, 85609 Garching, Germany

2 PSI Center for Neutron and Muon Sciences, Paul Scherrer Institut, CH-5232 Villigen PSI, Switzerland

3 Department of Physics, Changwon National University, Changwon, South Korea

4 Center for Quantum Materials and Superconductivity and Department of Physics in Sungkyunkwan University, 16419 Suwon, South Korea

CeAlGe crystalises in tetragonal structure I41md, where the spatial-inversion symmetry is broken, and is expected to exhibit Weyl fermions near a Fermi surface that becomes more stable by broken time-reversal symmetry [1]. It has been known that the magnetic ground state and relevant topological properties of CeAlGe depend on the chemical stoichiometry. For example, CeAlGe grown by the flux method yields 5 ~ 15% additional Al in the Ge site and exhibits a commensurate antiferromagnetic order below T = 5.1 K [2], whereas the crystal grown by floating-zone methods with 30 bar of Ar gas (p=30 bar) is resulted in stoichiometric composition and exhibits an incommensurate order below T = 4.4 K in which topological Hall effects are induced by external magnetic fields [3]. In this presentation, we show the experimental results of newly synthesised CeAlGe using the optical floating-zone furnace with lower Ar pressure of p=5 bar. Our neutron diffraction and electrical Hall transport experiments revealed that the topological magnetism is still stabilised with shorter periodicity. Furthermore, we performed electrical transport experiments under pressure up to 2 GPa. Given all experimental results obtained using flux-grown and two floating-zone-grown CeAlGe crystals, we will discuss the mechanism of topological magnetism with respect to the Kondo coupling strength.

[1] G. Chang et al., Physical Review B, 97, 01104 (2018)

[2] T. Suzuki et al., Science, 365, 377-381 (2019)

[3] P. Puphal et al., Physical Review Letters, 124, 017202 (2020)

E-mail of the corresponding author: so.shin@fz-juelich.de